DfR-QTM: A Software Package for the Analysis of QCM-D Data exploiting the Df-ratio

# General

With regard to the definition of variables and other background, the user is referred to ref. 1 or the manual of PyQTM.

DfR-QTM is a down-sized and modified version of the software package PyQTM.  PyQTM models data obtained with a QCM-D, based on the thickness of the layer and its viscoelastic parameters.  The scope of DfR-QTM is reduced compared to PyQTM.  The sample is a single homogeneous film with no roughness.  The bulk is a Newtonian liquid with density rbulk and viscosity hbulk (both set by the user, not fit parameters.)

DfR-QTM extends PyQTM with regard to the exploitation of the “Df ratio”, defined as /(f).  The conventional fitting algorithm as implemented in PyQTM is plagued by problems with non-unique solutions.  From a physical viewpoint, the model should have five free parameters, which turns out to be one parameter too many.  In particular, the algorithm has trouble distinguishing a thin, stiff film from a thick, soft film.  The problem is discussed in more depth in section 4 (see also ref. 2).

Assumptions are needed to obtain unique results.  DfR-QTM proposes a set of two such assumptions, which are

- The film thickness is much below the depth of penetration of the liquid, which allows for a Taylor expansion of the full equation predicting Df and DG (Eq. 1) to first order in df (leading to Eq. 2).

- The film’s elastic compliance, Jf, is much smaller than (whbulk)-1, meaning that the film is rather stiff (see the denominator in Eq. 4).

Both assumptions make sense for adsorbed proteins.  (They do not necessarily make sense for polymer brushes, because these may be dilute assemblies of chains, the softness of which may be comparable to the softness of the liquid.)  Assumptions a) and b) allow to estimate. Jf’ and  from the Df ratio (from /(f) in a model-free way (Eq. 6 and Fig. 1).  That brings the number of fit parameters down to three.  The standard errors are much reduced.  Actually, one may infer either Jf’ or  from the Df ratio and the let the other parameter be a fit parameter.  The fit runs well with four free parameters (but not with five).

Of course those assumptions amount to a compromise.  Moderate systematic deviations between the data and the fit are seen.  c2 is increased compared to the fit with five free parameters.  Still, DfR-QTM is more practical than PyQTM when the assumptions are justified.

# Mathematical background

The software implements the multilayer formalism (no perturbation analysis).  For films of arbitrary thickness, the equation predicting Df and DG is:

Eq. 1

For the meaning the variables see ref. 1.  The tilde denotes a complex parameter.  Taylor expansion of Eq. 1 to first order in df leads to

Eq. 2

Replacing Zf2 by Jf/f, and replacing Zbulk2 by ibulk leads to

Eq. 3

Constant density (rbulk = rfilm) was assumed in step 2.

Because the compliance, J, is the numerator in these expressions, rheological parameters inferred from QCM results are most conveniently discussed in terms of J (rather than G).  J = 0 leads to Sauerbrey-type behavior.  J is related to the slopes in plots of Df/n and DG/n versus n.  Remember that J is itself a function of n because of viscoelastic dispersion.

For the Df-ratio, Eq. 3 leads to 3

Eq. 4

Assuming Jfwhbulk << 1, this result simplifies to

Eq. 5

Fig. 1

DfR-QTM fits a straight line to a log-log plot of the apparent elastic compliance from Eq. 6 versus n.  The slope is the power-law exponent,  (Eq. 7a).  The intercept is the logarithm of Jcen.  Both may or may be not be free parameters in the subsequent fit.  If they are not, the number of free parameters of the model is reduced (from five to three of four).

Inverting this relation for an apparent Jf leads to

Eq. 6

This relation applies at all overtones (labeled by overtone order n) separately.  A few different values of Japp(n) are obtained, which allows to also infer the parameter , following Eq. 7 (see Fig. 1).

# Choices for the viscoelastic parameters, viscoelastic dispersion

Viscoelasticity is often quantified in terms of the shear modulus, G̃.  For the QCM, it is often convenient to use the compliance, J̃ = 1/G̃.  The reasons are discussed below Eq. 3.

For ease of interpretation, PyQTM offers the following sets of parameters: 
- J and J
- G and G
-  and 
- G and 
- |J̃| and tan()
- |G̃| and tan()
- |̃| and 1/(tan()

Importantly, the viscoelastic parameters depend on frequency.  This might create the impression that the problem was underdetermined because there are separates values of J and J (or of any of the other parameters in the list above) for every single overtone.  However, the frequency dependence of J and J usually is smooth (Fig. 2).  PyQTM assumes power laws of the form

Eq. 7

or (for instance)

Eq. 8

fcen is a frequency in the center of the accessible range.  The values of  and  depend on the choice of the parameters.

The loss tangent, tan(), is defined as tan()  GG  JJ  /.  The loss tangent is independent of whether viscoelasticity is quantified with G, J, or .  If the loss tangent has a peak at some frequency, the medium under study undergoes relaxations with rates in the range of the peak in tan().

| Fig. 2 The shear modulus of viscoelastic materials depends on frequency. The plot shows a typical rheological spectrum of a long-chain linear polymer in solution.4 The frequency scale extends over many decades, while the QCM only covers about one decade. In this limited frequency range, G(ω) and G(ω) can be approximated by power laws (dashed blue lines in A). For the QCM, the pair {J(ω),J(ω)} is more practical than the pair {G(ω), G(ω)} (B). from ref. 1. |  |
| --- | --- |

# The full set of five fit parameters often leads to non-unique fit results

Basically, the model has five free parameters, which are the thickness, the complex shear modulus (two parameters for the real and the imaginary part) and two power-law exponents, ' and '', quantifying viscoelastic dispersion.  It turns out that those five parameters often are one parameter too many.  Good matches between the model and the data can certainly be produced, but they can be produced in different ways.  For this particular case, a look at the raw data makes the problem transparent (Fig. 3).  Noisy data can often be well described with a straight line for Δf/n and a second straight line for ΔΓ/n.  Each of these lines contains two parameters, which are the offset and the slope.  A fifth parameter (needed to nail down the five free parameters of the viscoelastic model) would require to determine the curvature in plots of Δf/n or ΔΓ/n versus n with confidence.  That can sometimes be done for thick films (Fig. 3B), but not usually for thin films (Fig. 3A).  For thin films, the landscape of χ2 plotted versus the model’s parameters shows extended valleys.  In particular, the fit has difficulties in distinguishing between a thin, stiff film and a thick, soft film (green bars in Fig. 4).

| Fig. 3 For thin films (A), the fractional noise is too large to let a curvature in plots of Δf/n and ΔΓ/n versus n be determined reliably. Interpretation must rely on the offsets and the slopes (totaling in four parameters). If the model contains five parameters, the problem is underdetermined. For thicker films (B), the curvatures can be determined. Five model parameters can then be derived, as well. from ref. 2 |  |
| --- | --- |

On a mathematical level, there is no solution to this problem.  One may, however, make the assumption a) and b) from section 1.  These amount to a rather stiff film, located at the left edge of the green bars in Fig. 4 .

| Fig. 4 An analysis of the  landscape for the datasets shown in Figure 7B and C. The software prescribes values for the thickness in a certain range (0 to 10 nm) and fits the remaining parameters, which are Jf’, ’, Jf’’, and ’’. Given that the thickness is no longer a free parameter,  is larger than what is obtained with df as a free parameter.  is large when df is smaller than 2 nm, but is only marginally larger than the minimum value when df is larger than 2 nm. The fit compensates for a large thickness with a large J’ and finds a good match with the experimental data (green bars). The algorithm cannot distinguish between films that are either thin and stiff or thick and soft. from ref. 2 |  |
| --- | --- |

# Details and technicalities

Fig. 5 shows the user interface.  It is similar to the interface of PyQTM.  Comments (also on the internal machinery) follow as a list.

- The main extension compared to PyQTM is the combo box at the bottom center of the model frame.  The choices are  
a) DfR → none
      Do not exploit the Df-ratio.  DfR-QTM then runs similarly to PyQTM 
b) DfR → J' (recommended)
     Infer J' from the Df ratio but not β'.  The model underlining the fit then has four free parameters.  
     Uniqueness of the fit parameters then is not a severe problem.  
c) DfR → β'
     Infer β' from the Df ratio, but not J'.  
d) Infer both J' and β' from the Df ratio. 
     Leads to three free parameters.

- DfR internally always fits with the of parameters {J', J'', β' and β'}' as displayed in the edit fields.  Conversion to other choices for the parameters occurs after the fit.  The Model Parameters plot always displays the choice made in the combo box on the lower right of the Model frame.

- When the film thickness zero, viscoelastic parameters cannot be obtained.  DfR-QTM ignores those data points.

Fig. 5

The user interface of DfR-QTM

All fits use the current entries of the Model frame as starting values.  When these entries are changed, the content of Model Parameters plot may slightly change.

References:

(1)	Johannsmann, D.; Langhoff, A.; Leppin, C. Studying Soft Interfaces with Shear Waves: Principles and Applications of the Quartz Crystal Microbalance (QCM). Sensors 2021, 21 (10), 3490. https://doi.org/10.3390/s21103490.

(2)	Johannsmann, D.; Langhoff, A.; Leppin, C.; Reviakine, I.; Maan, A. M. C. Effect of Noise on Determining Ultrathin-Film Parameters from QCM-D Data with the Viscoelastic Model. Sensors 2023, 23 (3). https://doi.org/10.3390/s23031348.

(3)	Du, B. Y.; Johannsmann, D. Operation of the Quartz Crystal Microbalance in Liquids: Derivation of the Elastic Compliance of a Film from the Ratio of Bandwidth Shift and Frequency Shift. Langmuir 2004, 20 (7), 2809–2812.

(4)	Baumgaertel, M.; Schausberger, A.; Winter, H. The Relaxation of Polymers with Linear Flexible Chains of Uniform Length. Rheologica Acta 1990, 29, 400–408. https://doi.org/10.1007/BF01376790.

Other researchers define the Df ratio as DD[10-6]/(-Df/n).  DD is the shift in dissipation, where dissipation is defined as 2G/fres.  The term “Df ratio” is inherited from this definition.  For 5-MHz crystals DD[10-6]/(-Df/n) = DG/(-Df) / 2.5.  Some researchers is the term “acoustic ratio” instead of “Df-ratio”.

Rheological spectra are smooth because they are governed by relaxations, as opposed to resonances.  Resonance produce sharp peaks.